COUNTY OF ALAMEDA

ADDENDUM No. 1

to

RFQ No. 901884

### for

Chip Seal Program - Oil

Specification Clarification/Modification and Recap of the Networking/Bidders Conferences

## Held on April 16, 2020

This County of Alameda, General Services Agency (GSA), RFQ Addendum has been electronically issued to potential bidders via e-mail. E-mail addresses used are those in the County’s Small Local Emerging Business (SLEB) Vendor Database or from other sources. If you have registered or are certified as a SLEB, please ensure that the complete and accurate e-mail address is noted and kept updated in the SLEB Vendor Database. This RFQ Addendum will also be posted on the GSA Contracting Opportunities website located at http://www.acgov.org/gsa/purchasing/bid_content/ContractOpportunities.jsp.

Alameda County is committed to reducing environmental impacts across our entire supply chain.

If printing this document, please print only what you need, print double-sided, and use recycled-content paper.

The following Sections have been modified to read as shown below.  Changes made to the original RFP document are in bold print and highlighted, and deletions made have a strike through.

## BIDDER MINIMUM QUALIFICATIONS

    - Bidder shall be regularly and continuously engaged in the business of providing Chipseal PMRE and/or CRS2H or equivalent services for at least three (3) years.

    - Bidder shall possess all permits, licenses and professional credentials necessary to supply product and perform services as specified under this RFQ.

    - Bidder shall have experience in performing Chipseal PMRE and/or CRS2H or equivalent projects of similar scope, size, and intent for public organizations of a size equivalent to, or larger than, Alameda County.  This must be verifiable through references submitted with bidder’s response.

## SPECIFIC REQUIREMENTS

PMRE and/or CRS2H or equivalent shall be cationic type, polymer grade and conform to the following special provisions:

- MATERIAL

  - The polymer shall be added to either the asphalt or the emulsion at the location of the manufacturer.  The binder shall conform to the aggregate with ten percent (10%) maximum film stripping as tested by Caltrans Specifications, Section 302.

  - The polymer shall be either neoprene or a blend of butadiene and styrene.

  - The temperature of the polymer modified asphalt emulsion at the time of application shall be between one hundred thirty (130) degrees and one hundred eighty (180) degrees Fahrenheit.

  - PMRE and/or CRS2H or equivalent shall comply with all regulations of the Bay Area Quality Management District.

Materials furnished and references to section numbers under this Request for Quotation (RFQ) shall conform and/or refer to the State of California, Department of Transportation (Caltrans) Standard Specifications, dated May 2018 and any amendments thereto. County of Alameda Specifications may override the Caltrans Standard Specifications on some occasions, as advised by the County. In the event of a conflict between the Caltrans Specifications and the County Specifications, the latter shall take precedent. Reference copies of the Caltrans Standard Specifications are available online at:

http://ppmoe.dot.ca.gov/hq/esc/oe/construction_contract_standards/std_specs/2018_StdSpecs/2018_StdSpecs.pdf

Please refer to section 37 – Bituminous Seals on this pdf document.

- TRUCKS

a.	Contractor shall be required to provide two (2) twenty-five (25) ton capacity trucks, and trailer units with a capacity between 20 (twenty) and 22 (twenty-two) tons, both equipped to spread.

4.	BIDDER

a.	Bidder shall have experience in performing Chipseal PMRE and/or CRS2H or equivalent projects of similar scope, size and intent for public organizations of a size equivalent to, or larger than, Alameda County.  This must be verifiable through references submitted with bidder’s response.

    - QUALITY CONTROL

      - Contractor shall maintain a quality control system that is in compliance with the Bay Air Area Quality Management District and shall provide records that all materials submitted for use conform to contract requirements. At its discretion, the County shall test any or all materials for compliance to the specifications listed in this RFQ.

      - Contractor shall sample and perform all of the following tests for every production batch of PMRE AND/OR CRS2H supplied to the County:

| Test | Test Method | Requirements |
| --- | --- | --- |
| Viscosity at 122 Degrees | AASHTO T‐59 | 100‐250 Seconds |
| Settlement, Five (5) Days | AASHTO T‐59 | 5% Maximum |
| Storage Stability Test One Day | AASHTO T‐59 | 1% Maximum |
| Sieve | AASHTO T‐59 | 0.3% Maximum |
| Demulsibility | AASHTO T‐59 | 60% Min.‐95% Max |
| Particle Charge | N/A | Positive |
| Ash Content | ASTM D‐3723 | Maximum |

    - TEST ON RESIDUE

      - Penetration

| Test | Test Method | Requirements |
| --- | --- | --- |
| Seventy‐Seven (77) Degrees | AASHTO T‐49 | 40‐65 Fahrenheit, 100g, 5 Seconds |

      - Ductility

| Test | Test Method | Requirements |
| --- | --- | --- |
| Seventy‐Seven (77) Degrees | AASHTO T‐51 | 40 cm Minimum Fahrenheit, 5cm/Minimum |
| Softening Point Degrees | AASHTO T‐53 | 115 Minimum Fahrenheit |
| Residue | California Test 331 | 65% Minimum |
| Torsional Recovery | California Test 332 | 18% Minimum |

    - DELIVERY TESTING REQUIREMENTS

      - Contractor shall adhere to the following delivery requirements:

        - Supply “Through the Boot” samples of PMRE AND/OR CRS2H for testing purposes. Samples will be taken when approximately one half of the tank load has been depleted.

        - Deliver the PMRE to various roads in unincorporated areas of Alameda County. Road locations may be deleted or added at the request of the Road Department, therefore the quantities are approximate. No minimum or maximum is guaranteed or implied. Contact person in the Public Works Road Department is the Field Maintenance Supervisor, Telephone (925) 803-7013, who will coordinate the deliveries.

        - Provide two (2) twenty-five (25) ton capacity trucks and trailer units, both equipped to spread materials at the work site.

        - Provide materials adequate to support an estimated production rate of fifty (50) tons per day based on a four (4) day work week (Monday through Thursday). There may be times the rate will decrease to twenty‐five (25) tons per day or less.

        - Provide two (2) hours free spread time per truck and trailer.

        - PMRE shall be manufactured from asphalt, a rejuvenator agent and a polymer. The asphalt emulsion shall be a polymer modified rejuvenating emulsion with a polymer rejuvenating agent and shall meet the below listed specifications.

        - The Bidder shall sample and perform, as a minimum, all of the following tests for every production batch of PMRE supplied to the County:

| Tests on Emulsion |
| --- |
| Specification Designation | Test Method | Requirement |
| Viscosity SFs @ 122⁰F (50⁰C), sec. | AASHTO T 59 | 50 - 350 |
| Sieve, % | AASHTO T 59 | 0.10 maximum |
| Settlement, 5 days, % | ASTM D 244 | 5.0 maximum |
| pH | ASTM E 70 | 2.0 – 5.0 |
| Oil Distillate, wt. % | ASTM T 59 | 0.5 maximum |
| Residue by Evaporation, wt. % | California TM 331 | 65 minimum |
| Tests on Residue by Evaporation |
| Specification Designation | Test Method | Requirement |
| Penetration @ 39.2⁰F (4⁰C), 200g, 60s, 0.1mm | AASHTO T 49 | 40 minimum |
| Viscosity @ 140⁰F (60⁰C), P | ASTM D 2171 | 5000 maximum |
| Elastic Recovery(1,2), 50⁰F (10⁰C), % | ASSHTO T301 | 60 minimum |
| OR Torsional Recovery(1,3), % | California TM 332 | 45 minimum |
| Tests on Rejuvenating Agent |
| Specification Designation | Test Method | Requirement |
| Viscosity @ 140⁰F (60⁰C), cSt | ASTM D 2170 | 50 – 175 |
| Flash Point, COC, ⁰F | ASTM D 92 | 380 minimum |
| Saturates, wt. % | ASTM D 2007 | 30 maximum |
| Asphaltenes, wt. % | ASTM D 2007 | 1.0 maximum |
| Tests on Rejuvenating Agent RTFO Residue |
| Specification Designation | Test Method | Requirement |
| Weight Change, wt. % | ASTM D 2872 | 6.5 maximum |
| Viscosity Ratio (RTFO/Original) | ASTM D 2170 | 3.0 maximum |

(1) Choose either Elastic Recovery or Torsional Recovery as a test.

(2) Elastic Recovery @ 50⁰F (10⁰C): Hour glass slides, pull to 20cm, hold 5 minutes then cut, let sit 1 hour.

(3) Torsional Recovery shall include the first 30 seconds.

| Test on Emulsion | Method | Polymer Modified Rejuvenating Emulsion Specifications |
| --- | --- | --- |
| Viscosity @77 (SFS) | ASTM D244 | 75 ‐ 350 |
| Residue, w%, minimum | ASTM D244 | 67 |
| pH | ASTM E70 | 2.0‐5.0 |
| Sieve, w%, max | ASTM D244 | 0.1 |
| Oil distillate, w%, max | ASTM D244 | 0.5 |
| Test on Residue(1) | Method | Specifications |
| Viscosity @ 140°F, P, maximum | ASTM D2170 | 2000 |
| Penetration @ 39.2°F, minimum | ASTM D5 | 40 |
| Elastic Recovery on residue by distillation(1,2) , %, minimum | AASHTO T59, T301 | 70 |
| Test on Latex(3) | Method | Specifications |
| Tensile strength, die C dumbbell, psi, minimum | ASTM D412 | 500 |
| Swelling in rejuvenating agent, % maximum; 48 hours exposure @ 104°F | ASTM D471(4) Modified | 40% intact film |

| Test on Rejuvenating Agent | Method | Specifications |
| --- | --- | --- |
| Flash point, COC , °F | ASTM D92 | > 380 |
| Hot Mix Recycling Agent Classification | ASTM D4552 | See Section II |

1 Exception to AASHTO T59: Bring the temperature on the lower thermometer slowly to 350o F plus or minus 10o F. Maintain at this temperature for 20 minutes. Complete total distillation

in 60 plus or minus 5 minutes from first application of heat.

2 Elastic Recovery @ 10o C (50o F): Hour glass sides, pull 20 cm, hold 5 minutes then cut, let sit 1 hour.

3 Latex films shall be cured at 75°F and 50% relative humidity for 14 days prior to cutting or molding specimens Suitable substrate for film formation shall be polyethylene boards, silicone

rubber sheeting, glass, or any substrate which produces a cured film of uniform cross‐section.

4 Report mass increase as a percent by weight of the original latex film mass upon exposure of films to the recycling agent.

      - The recycling agent shall meet the following specifications:

| Test | Recycling Agent Specification |
| --- | --- |
| Viscosity, 140F, CST | 50‐175 |
| Flash Point, F, COC | 380 Min |
| Saturate, % by wt. | 30 Max |
| Asphaltenes | 1.0 Max |
| Test on Residue | Recycling Agent Specification |
| Weight Change, % | 6.5 Max |
| Viscosity Ratio | 3 Max |

        - Contractor shall use California test method CA‐331 when performing Torsional Testing for recovery of residue. Torsional recovery measurement shall include the first thirty (30) seconds.

        - The asphalt shall be made from one hundred percent (100%) crude oil, originating from what is known as the Vacca Tar Sand formation in Ventura County.

        - The rejuvenator agent shall be RA‐1, manufactured by the San Joaquin Refining Company or Tricor Refining Company.

## DELIVERABLES / REPORTS

    - Vendor must be able to furnish most current Material Safety Data Sheet (MSDS) for the materials furnished.

    - Bidder shall submit with their bid, a certified lab report showing that PMRE AND/OR CRS2H or equivalent material meets specifications according to the United States Patent No.5, 180.428 and all other applicable specifications listed herein.  Lab report shall be no more than forty-five (45) days old and shall be from an independent professional testing laboratory, accredited in accordance with ASTM D-3666.

Responses to Written Questions

** There were no questions submitted prior to the April 17th, 2020 deadline. **

The following participants attended the Bidders Conferences:

|  | Company Name / Address | Representative | Contact Information |
| --- | --- | --- | --- |
|  | Reed and Graham 690 Sunol St, San Jose, CA 95126 | Cliff Clowers | Phone: (408) 287-1400 |
|  |  |  | E-Mail: cliff@rginc.com |
|  |  |  | Prime Contractor: Yes |
|  |  |  | Subcontractor: No |
|  |  |  | Certified SLEB: No |
|  | Reed and Graham 690 Sunol St, San Jose, CA 95126 | Peter Fitzpatrick | Phone: (408) 287-1400 |
|  |  |  | E-Mail: peter@rginc.com |
|  |  |  | Prime Contractor: Yes |
|  |  |  | Subcontractor: No |
|  |  |  | Certified SLEB: No |